**Terratex Collection**

Terra Canvas 310 FR

310g/m2 polyester fabric with special resin coating, ideal for theatrical or museum backdrops. Environmentally friendly and fire retardant.

Material: 78% PES / 22% ACRYLATE

Weight: 310 g/m2

**Features:**

PVC free

No fraying

Crease resistant

Good flatness

Recyclable under code nr. 1 (PET)

**Applications:**

Theatre backdrops

Display frame systems

Art reproduction

Exhibitions

Banners

Apllications requiring ecological approval

**Product attributes:**

Compatibility with Solvent, Eco-solvent, Uv and Latex Inks

 FR available – B1

 Indoor

Up to 5 meters