**Print Collection**

Blockout

Opak X

Material: 80% PVC / 20% PES

Weight: 650 g/m2

**Features:**

High mechanical resistance

Opacity

 Double side print

**Applications:**

Large format advertising for facades

 Signage (Double side print)

Banners (Double side print)

**Product attributes:**

Compatibility with Solvent, Eco-solvent, Uv and Latex Inks

FR available – B1

Indoor and Outdoor

Up to 5 mters