**Walltex Collection**

Print N Wall

330g/m2 self-adhesive PVC coated cotton fabric, with different embossings for indoor decoration.

Material: 64% PVC / 36% COTTON

Weight: 330 g/m2

**Features:**

Quick application without special knowledge

Strong adhesion to various types of surfasse

Different textures available

Excellent printability

**Applications:**

Indoor Decoration

Wall coverings

In-store display

Exhibitions

**Product attributes:**

Compatibility with Solvent, Eco-solvent, Uv and Latex Inks

FR available – B1

Indoor