**Sublitex Collection**

Tex Stretch 180 FR

180g/m2 polyester knitted fabric with special PU back coating. Environmentally friendly and fire retardant.

Material: 42% PU / 58% PES

Weight: 180 g/m2

**Features:**

High elasticity

Easy to print

High quality colour reprodution

**Applications:**

3D Buildings

Frames

Indoor Decoration

Store design

Exhibitions

**Product attributes:**

Transfer and direct dye sublimation

Compatibility with UV and Latex Inks

FR available – B1

Indoor